## Slide 1: Liquid metal divertors
Jan Čečrdle
Mariánská XIV
11.1.2021

## Slide 2: Outline
Introduction to liquid metal divertors
LMD simulations
Current work
Future plans

## Slide 3: Divertor overheating
ITER divertor steady state heat flux must be <16 MW/m2 (DEMO <15 MW/m2)
85 % of the power must be radiated (impurity seeding)
For DEMO 98 %!!!
© R. Pitts

## Slide 4: Liquid metal plasma facing components
Replace the solid plasma facing component with a liquid
No melting
No recrystallization
Self-restoration
Vapour shielding
© Tristar Pictures
© STUDIOCANAL
>
?

## Slide 5: Disadvantages of liquid metals?
Fluidity
High erosion rate
Fuel retention
High SOL and core radiation
© R. E. Nygren

## Slide 6: No crystalline lattice versus fluidity
A bulk substrate material needed (tungsten)
Tungsten mesh (felt)
3D printed materials
Bulks with trenches
Thermally induced forces
Flowing metal
© P. Rindt
© V. A. Evtikhin
© Z. Li

## Slide 7: Vapor shielding
Cooling effects:
Latent heat
  Sputtered atoms
  Evaporation
Line radiation
Ionisation
© T. W. Morgan

## Slide 8: Which metals can be used
Consider:
Melting point
Boiling point
Evaporation rate
Atomic mass

## Slide 9: Tin or lithium
Lithium:
Low Z
High outflux
Tin:
High Z
Low outflux
Sn/Li alloy -> best of both
Only Li evaporated
Lower outflux compared to Li

## Slide 10: Radiation in plasma
Lithium:
Weak vapour shielding per atom
High concentration in core plasma possible >20%
Tin:
Very strong vapour shielding per atom
NO tin in core plasma (<0.03 %)
© T. Pütterich
Radiation cooling factor for various elements

## Slide 11: Two approaches
Vapour shielding regime (lithium)
Equilibrium of steady state heat flux conduction and vapour cooling
Transients mitigated by increased erosion.
Lithium transport control
Fail safe regime (tin)
In steady state business as usual
Vapour cooling serves only as a fail safe for transient heat events
Even a tiny amount eroded can cause problems

## Slide 12: Edge localised modes
ITER ELMs energy fluence 66 MJ/m2s-1/2 just below the flash melting point
SPARC ELMs comparable to ITER with 4x smaller vessel
ELMs can ‘‘burn’’ through impurity seeding
© J. R. Walk

## Slide 13: Vapor shielding
Electron density and temperature crucial
Cooling power can easily change by a factor of 100
Very beneficial for ELMs

## Slide 14: Effect of electron temperature
H-mode divertor plasma with DEMO like parameters
Steady state heat flux
350 MW/m2
Peak heat flux during ELMs
≈ 1 GW/m2
Electron density
1e21 m-3 to 3e21 m-3
Electron temperature
10 eV or 30 eV

## Slide 15: Liquid metal versus tungsten divertor
Lithium heat conductivity lower
Vapor shielding suppresses ELM spiking
Vapor shielding slows down temperature increase (eventually saturates)
How to deal with poor LM thermal conductivity?
Surface temperature

## Slide 16: Liquid metal versus tungsten divertor
Lithium heat conductivity lower
Vapor shielding suppresses ELM spiking
Vapor shielding slows down temperature increase (eventually saturates)
Surface temperature

## Slide 17: AUG liquid metal experiment simulations
Currently finalizing a new python version of the code
Model referential discharges
How much tin will be evaporated?
How far can we go?
Fig.: Model of the tested target. Dimensions in mm. [Scholte]
Discharge parameters

## Slide 18: Effect of high density
High density plasma may erode the surface significantly by sputtering only
Cannot be counter measured by stronger conductive cooling
Sheath versus conduction limited regimes
Sputtering in detached plasma?

## Slide 19: Effect of high density
High density plasma may erode the surface significantly by sputtering only
Cannot be counter measured by stronger conductive cooling
Sheath versus conduction limited regimes
Sputtering in detached plasma?

## Slide 20: Evaporation suppression
Evaporation dependent on surface temperature
AND partial pressure
Partial pressure in all cases assumed equal to zero
Is this true in high recycling/detached regimes?
OR

## Slide 21: Thank You very much